## Slide 1
Superconductivity Lecture 5: Josephson Effect

## Slide 2
Supercurrent driven by phase difference
(not potential difference)
1st Josephson relation
Ic

## Slide 3
weak link (barrier)
What’s a Josephson weak link?
Many options!
Insulator: SIS Tunnelling
Normal metal: SNS Proximity
Superconducting: SsS Constrictions
…
But CPR must remain single-valued
Depending on material & size, CPR can deviate from standard

## Slide 4
Phase → Position
Voltage → Velocity
Bias current → Driving force (the tilt)
=
Josephson eqns:
Current–Phase relation → V = 0 (steady state)
Voltage–Phase relation
→ V ≠ 0 (dynamic regime)
Periodic Josephson potential
Tilted washboard analogy

## Slide 5
RCSJ Model
Phase (here written as δ) → Position (x)
Voltage → velocity
Capacitance → Mass (m)
Friction → Conductance (1/R)
Bias current → Driving force (Fd)
What happens in the JJ when ?
JJ
JJs have R & C (high if SIS, small if SNS). But we ignore R & C if (why?)
An ac voltage appears across the circuit (parallel to the JJ)
→ 3 different currents: 1 AC supercurrent + 2 normal (unpaired es) channels

## Slide 6
Making sense of I-Vs with the tilted washboard
Phase → Position
Voltage → velocity
Capacitance → Mass
Friction → Conductance
Bias current → Driving force
(escape)
(re-trap)
Underdamped junction
Hysteresis in IV
Overdamped junction
No hysteresis in IV

## Slide 7
Making sense of I-Vs with the tilted washboard
Phase → Position
Voltage → velocity
Capacitance → Mass
Friction → Conductance
Bias current → Driving force
SIS (Nb/Al-AlOx/Nb)
SNS (Nb/Au/Nb)
Nb
Nb
Au
Au
Which JJ would have a larger hysteresis in their IV? Why?
https://doi.org/10.1515/9783110456806-012
Dieter Koelle et al
https://doi.org/10.1103/PhysRevB.77.165408
Angers, Chiodi, et al

## Slide 8
RCSJ Modelling
Matthijs Rog (Lahabi lab)
Measured I-V as a function of field
Simulated RCSJ
(neural network)

## Slide 9
Weak Link
Back to dynamic regime:
; = GHz / mV
Josephson supercurrent oscillates at
(time-averaged voltage)
When V≠ 0, an AC supercurrent develops across the JJ
Oscillating supercurrent → Oscillating EM field
In what frequency range?
The voltage across JJ can vary from nV up to 10s of mVs
JJ generates microwaves

## Slide 10
Weak Link
Using JJs as high-freq generator
= GHz / mV
“Imaging of coins in a mail envelope using a 0.537-THz beam generated by a 62-μm-wide mesa that is operated in the high-bias regime91. …fringes caused by reflections between the paper sheets of the envelope are visible in the blue region of the image”
Closing the so-called THz gap (0.5–1.3 THz) with
intrinsic JJs in cuprates
The reverse?
DC supercurrent → Generates RF

## Slide 11
Weak Link
Shapiro Steps:
open-ended coax (GHz antenna)
JJ (Measured in DC)
Step height: V =
Step width microwave power ( magnitude of induced Irf)
Quantized steps in I-V, when JJ irradiated by microwaves
Standard unit of voltage

## Slide 12
Fraunhofer Pattern (other considerations)
Blom,… Lahabi ACS NANO (2020)
Long diffusive JJ

## Slide 13
Hart, S. et al. Nature Phys. 10 (2014)
Dependence on the spatial distribution of critical current density Jc (x)

## Slide 14
Transport channel < 80 nm
Spin-triplet rim currents (an unsolved puzzle)
Fermin,… Lahabi Nano Lett. (2022)

## Slide 15
π-junction
0-junction
Different classes of JJs (according to their potential)
How does Ic (B) of a π-JJ differ from a 0-JJ? (see homework)

## Slide 17
Transport channel < 80 nm

## Slide 18: Switching the phase of triplets using spin texture: 0-0 to 0-π
Bz
B in-plane 80 mT
No vortex → no supercurrent
By
B in-plane = 10 mT
Asymmetric pattern: 0-π SQUID

## Slide 19
Grain boundary JJs in cuprate SC films
Which GB config makes a π-JJ?
Notes: Thank you for the introduction, now let me get started. Hello everyone, for the one who is unfamiliar with the talk-too much face: I’m nick Nick Groen and I have been working on the manufacturing and measuring of three-dimensional superconducting nanostructures.
Thank you for the kinded worded introduction, for those who don’t know me, I’m Nick Groen and for the last several months I have been working on the fabrication of superconducting three-dimensional nanostructures.

## Slide 20
0-π Junctions: zig-zag junctions formed between facets of a YBCO crystal & Nb film

## Slide 21
0-π Junctions: SFS Junctions with 0 and π segments

## Slide 22
0-junction
-junction
Homework:
What would I-V sweeps of a -junction looks like?
More exotic cases: Phase batteries
Spontaneous TRSB

## Slide 23: Bonus slides: Time-reversal symmetry breaking in Josephson devices

## Slide 24
Time-reversal Symmetry (TRS)
CPR Measurement
Matthijs Rog & Julian Doorn
(Lahabi Lab)
Δ=

## Slide 25
Time-reversal Symmetry (TRS)
Δ=
CPR measurement
Matthijs Rog
& Julian Doorn

## Slide 26
TRS breaking: Josephson devices
- Junction
External magnetic field + Spin-orbit + gating
Superconducting rectifiers and diodes